G999999

G999999 (Don’t change this number)

Band-gap tuning of a MoS2 monolayer by mechanical strains

Soon-Dong Park† and Sung Youb Kim

School of Mechanical and Advanced Materials Engineering

Ulsan National Institute of Science and Technology (UNIST), Ulsan 689-798, Republic of Korea

†E-mail: simao@unist.ac.kr (presenter’s email)

Extended Abstract

(10pt, Times New Roman) After the discovery of graphene and the exfoliation technique for extracting single layer from the bulk sample, a very large number of the experimental and theoretical studies have been carried out about the two-dimensional nanomaterials [1-3]. Until now, the most widely studied two-dimensional material is the graphene, owing to the unusual properties such as a considerable mechanical strength [4] and ultra-high mobility [1]. Recently, other two-dimensional nanomaterial, molybdenum disulfide, have also attracted significant interest and possessed the great potential for a variety of applications. Radisavljevic et al. reported the new application of MoS2 monolayer for Metal-Oxide-Semiconductor Field-Effect Transistor channel using halfnium oxide (HfO2) with the mobility of 200 cm2/Vs, indicating that MoS2 monolayer is able to be used as channel of MOSFET [5]. The mobility of carrier is the most important factor for application of MOSFET channel. The conventional semiconductor materials show that the electron mobility decreases as the band gap increases, and similar trends have been shown for carbon nanotubes (CNTs) and graphene nanoribbons (GNRs). According to the previous calculations [6, 7], the strain induced band-gap opening in graphene. In this work, we introduce strain for controlling band gap energy of MoS2 monolayer to enhance the mobility.

The electronic structure of MoS2 monolayer has been computed for each deformed configuration by using the density functional theory method (DFT) implemented in Vienna ab-initio simulation package (VASP) [8-10].

s

Fig. 1. The variation of the band gap energy with (a) biaxial, (b) pure shear, (c) uniaxial x and (d) uniaxial y strain, the solid circles and open circles denote indirect and direct band gap, respectively. The strain direction is shown in the left corner of each figure.

Table 1. Cohesive energy (Ec), lattice constant (a), bulk modulus (B) and elastic constants (C11, C12, C44) calculated with the new parameter sets.

|  | Ni-Ti | Ti-C |
| --- | --- | --- |
|  | Exp.[15] | First principles [16] | SMA [16] | MEAM [1] | This work | Exp. [17] | First principles [17] | This work |
| Ec(eV) | - | 5.02 | 5.02 | 5.02 | 5.02 | 6.9 | 6.9 | 6.9 |
| a(Å) | 3.02 | 3.01 | 3.01 | 3.01 | 3.01 | 4.33 | 4.42 | 4.42 |
| B(GPa) | 140 | 158 | 158 | 149 | 158 | 242 | 242 | 242 |
| C11(GPa) | 162 | 178 | 205 | 139 | 177 | 513 | 489 | 522 |
| C12(GPa) | 129 | 148 | 136 | 154 | 148 | 106 | 110 | 102 |
| C44(GPa) | 35 | 49 | 49 | 128 | 106 | 178 | 126 | 129 |

The total energy E of a system of N atoms in the MEAM is given by the form [7-10]

.						 (1)

where the embedding function Fi is the energy to embed an atom of type i into ~

Acknowledgement (If you don’t need to acknowledge, remove this part.)

(10pt, Times New Roman) This work was supported by Basic Science Research Program through the National Research Foundation of Korea (NRF) funded by the Ministry of Education, Science and Technology (Grant no. 2011-003137).

References

1.  K. S. Novoselov, A. K. Geim, S. V. Morozov, D. Jiang, Y. Zhang, S. V. Dubonos, I. V. Grigorieva, and A. A. Firsov, Science 306, 666 (2004).

2.  K. S. Novoselov, A. K. Geim, S. V. Morozov, D. Jiang, M. I. Grigorieva, S. V. Dubonos, and A. A. Firsov, Natrue 438, 197 (2005).

3.  Y.B. Zhang, Y. W. Tan, H. L. Stromer, and P. Kim, Nature 438, 201 (2005).

4.  C. Lee, X. D. Wei, J. W. Kysar, and J. Hone, Science 321, 385 (2008)

5.  B. Radisavljevic, A. Radenovic, J. Bribio, V. Giacometti, and A. Kis, Nature Nano 6, 147 (2011).

6.  G. Gui, J. Li, and J. X. Zhong, Phys. Rev. B 78, 075435 (2008).

7.  G. Cocco, E. Cadelano, and L. Colombo, Phys. Rev. B 81, 241412(R) (2010).

8.  G. Kresse and J. Hafner, Phys. Rev. B 48, 13 115 (1993).

9.  G. Kresse and J. Furthmuller, Comput. Mater. Sci. 6, 15 (1996).